Combination Agitator Flange and Plug

Specification (2NCF)

# Closing Instructions

COMBINATION AGITATOR FLANGE

MATERIAL:			Nylon 6/6

GASKET:			2” White EPDM

HEAT RESISTANCE:	350º @ 15 Minutes (Max)

THREADS:			2” ISO 228/1 External Thread

1 ½” NPSM Internal Thread

TORQUE:			20-22 ft-lbs.

1 ½” AGITATOR PLUG

MATERIAL:			Nylon 6/6

GASKET:			1 ½” – 130 White EPDM O-Ring

THREADS:			1 ½” NPSM External Thread

TORQUE:			8-12 ft-lbs.

Patent #:  7318668