Please be advised that the following information for the certification and process, regarding the Electro deposition of Cathodic Elpo Paint, will be used for agitators supplied by Woodman Agitator, Inc. to any facility requesting Cathodic Elpo Paint (E-Coat).

Name:	Woodman Agitator #44 E-Coat

Woodman Agitator will certify #44 E-Coat:

1.	N.S.S. To ASTM B117

500 hours

2.	Red rust less than 3 mm.

Pullback @ scribe (500 Hrs)

3.	Tape adhesion

No lifting @ scribe (500 Hrs)

No peeling @ scribe (500 Hrs)

4.	MIBK Cure Test (Methyl Isobutyl Keytone)

40 Double Rubs - Pass

No softening

5.	Film thickness 1 mil min.

Woodman Agitator will certify that the parts will meet this specification.  Acceptance criteria are zero discrepancies.

WOODMAN AGITATOR #44 E-COAT:

Coating:  PPG 699-484 - Tin Free E-Coat

Color:  Black

Process:  Aqueous clean

Zinc phosphate

Black E-Coat

Please note that during each step of the process, many quality-initiated controls are implemented to insure compliance during the particular step.  The specific controls for each step (i.e. solutions, pH/acidity levels, conductivity parameters) are proprietary information.

#44 E-Coat Spec.doc 1-1-2018

This document is confidential and shall not be distributed without the written consent of

Woodman Agitator, Inc.

www.woodmanagitator.com